The linear stability of a compositional plume in the presence of material diffusion

Khaled Suleiman AL-Mashrafi

Department of Mathematics and Statistics, College of Science, P.O. Box 36

Sultan Qaboos University, Muscat, Sultanate of Oman, E-mail:    p001175@squ.edu.om

One of the problems the iron casting industry faces is the appearance of freckles in iron bars leading to their weakness. When iron ore is poured into ingots the trapped air escapes in the form of thin air channels which when the iron bar solidifies appear as very thin black strips along the iron bar. These air pockets lead to a weakness in the iron bar.  Experiments of directional solidification using fluid alloys chilled from below showed that the formation of these channels is a result of instability of a mushy layer that forms at the bottom of the fluid alloy. These channels are now termed compositional plumes and are found to occur in a variety of situations in geophysics and the environment in addition to industry. It is then of importance to study the dynamics of these plumes. Recent work has shown that a single plume is unstable indicating that it can break up into blobs or widen and become bigger.

The studies on the dynamics of compositional plumes use the equations of conservation of mass, and conservation of momentum in the presence of Boussinesq approximation together with equations of heat, concentration of light material, and state. In particular, we examine the stability of a fully developed plume rising in a fluid of larger dimensions of different material composition. The dimensionless width of the plume,  , the Grashoff (Reynold) number  ( =   , where  and  are units of velocity and length , respectively , and   is the kinematic viscosity ), the Prandtl number,   ( , where   is the thermal diffusivity)  and the Schmidt number,  (=  , where   is the material diffusion) govern the stability of the plume. The stability is investigated in the parameter space ( ) for small values of the Grashoff (Reynold) number. The work extends previous stability analyses to include the material diffusion. It is shown that the presence of material diffusion has a stabilizing influence except in a small range of the Schmidt number. However, overall effect of material diffusion is tends to stabilise the plume with the consequences that the growth rate is reduced but the plume is remains unstable. Moreover, it was found that the influence of material diffusion is independent of the type of the mode considered.   The results are presented in graphical form in the parameter space and their significance is discussed.

- Copley, S. M., Giamel, A. F., Johanson, S. M.  and  Hornbecker, M. F. 1970 The origin of freckles in unidirectionally solidified casting. Metall. Trans. 1, 2193-2204.

- Eltayeb, I.A. and Hamza, E.A. 1998 Compositional convection in the presence of rotation. J. Fluid Mech. 354, 277-299.

- Eltayeb, I.A., Hamza, E.A, Jervase, J.A., Krishnan, E.A. and Loper, D.E., 2004. Compositional convection in the presence of a magnetic field. I. A single interface. Proc. R. Soc. Lond.A, 460, 3505-3528

- Eltayeb, I. A. and Loper, D. E. 1991 On the stability of vertical double-diffusive interfaces. Part1. A single plane interface. J. Fluid Mech. 228, 149-181.

- Eltayeb, I. A. and Loper, D. E. 1994 On the stability of vertical double-diffusive interfaces. Part2. Two parallel interfaces. J. Fluid Mech. 267, 251-271.

- Eltayeb, I. A. and Loper, D. E. 1997 On the stability of vertical double-diffusive interfaces. Part3. Cylindrical interfaces. J. Fluid Mech. 353, 45-66.

- Howard, L.N. and Veronis, G., 1992 Stability of salt fingers with negligible diffusivity.  Journal of Fluid Mechanics.  239, 511 – 522.

- Huppert, H.E., Buffett, B.A., Lister, J.R. and Woods, A.W. (1992) "Solidification and convection in the core of the Earth", In: Interactive Dynamics of Convection and Solidification, eds. S.H. Davis, H.E. Huppert, U. Müller and M.G. Worster, Kluwer Academic, pp. 265-267

- Loper, D. E. 1983 Structure of the inner core boundary. Geophys. Astrophy. Fluid Dyn.  25 , 139-155.

- Loper, D. E. and Roberts, P. H. 1983 Compositional convection and the gravitationally powered dynamo. In stellar and Planetary Magnetism ( ed. A. M. Soward) , pp. 297-327. Gordon and Breach.

- Loper, D. E. (ED.) 1987 Structure and dynamics of partially solidified systems. Matinus Nijhoff.

- Morgan, W. J., 1972 . Plate motions and deep mantle convection. Studies in Earth and Space Sciences , Geol. Soc. Am. Mem., 132 , 7-22.

- Wettlauffer, H. K. , Worster, M. G. and Huppert, H. E. 1997 Natural convection during solidification of an alloy from above with application to the evolution of sea ice. J. Fluid Mech. 244, 291 – 316.

- Worster, M. G. 1986 Solidification of an alloy from a cooled boundary. J. Fluid Mech. 167, 481-501.

- Worster, M. G. 1992 Instabilities of the liquid and mushy regions during solidification of alloys. J. Fluid Mech. 237 , 649 – 669.

- Worster, M. G. 1997 Convection in mushy layers. Annu. Rev. Fluid Mech. 29, 91 – 122

- Anderson, D.M. & Worster, M.G. 1995 Weakly-nonlinear analysis of convection in a mushy layer during the solidification of alloys. J. Fluid Mech.  302, 307—331